## Slide 1: Large Anisotropic Magnetoresistance and Magnetic properties of Single Crystalline, Tb2Al3Si2
Yash Anand, Ram Kumar, Shanta Saha, Johnpierre Paglione
Maryland Quantum Materials Center,
University of Maryland, College Park
APS March Meeting 2024 W23.00012

## Slide 2: Outline:
Background
Crystal Structure: X-ray Diffraction
Magnetism in Tb2Al3Si2
Transport Properties: Anisotropic Magnetoresistance
Summary
APS March Meeting 2024 W23.00012

## Slide 3
https://doi.org/10.1016/j.jssc.2005.04.021
Background
APS March Meeting 2024 W23.00012

## Slide 4: Crystal Structure: XRD
Name x y z occ.
Tb 4 0.61905( 14) 0.00000( 0) 0.32200( 21) 0 .473( 0) ~ 0.50
Si 4 0.90435( 54) 0.00000( 0) 0.35971( 80) 0.483( 0) ~ 0.50
Al 2 0.00000( 0) 0.00000( 0) 0.00000( 0) 0.259( 0) ~ 0. 25
Al 4 0.30098( 63) 0.00000( 0) 0.12840( 84) 0.515( 3) ~ 0. 50
Lattice parameters:
a=10.179(1) Å, b=4.038(1) Å , c= 6.600(2) Å and  =  = 90 , = 101.2 (1)
b-axis
1mm
b-axis
APS March Meeting 2024 W23.00012
https://www.topologicalquantumchemistry.com/#/detail/92448

## Slide 5
Tn1 ~ 13K
Tn2 ~ 8K
1.8K
3K
5K
7K
10K
15K
Magnetic Properties: H || b
APS March Meeting 2024 W23.00012
Notes: Small mag field, 2 transitions around 13K and another at 8K
Spin glass features because ZFC and FC bifurcation
First plot full sweep but others are only first quardanent
At different temperatures there is a hysteresis which shifts towards low fields as temperature increase, showing complexity of magnetic structure

## Slide 6
Magnetic Properties: H ⟂ b
APS March Meeting 2024 W23.00012
Notes: When Hperp to b shows further complexity in magnetic structure, as you can see from the MvH plot.

## Slide 7
Transport Properties
APS March Meeting 2024 W23.00012
Notes: No report on magnetoresistnac, we see the same transition at 13K and 8K as we saw in the magnetization. Even though it looks more complex in resistivity. Along different field orientation we see different response in resistivyt.

## Slide 8
Magnetoresistance
APS March Meeting 2024 W23.00012
Notes: Same orientation as the resistivyt we measured the resistivity as a function of field and calculated the magnetoresistance.

## Slide 9
Summary
Thank you so much for your attention!
APS March Meeting 2024 W23.00012
We grew large single-crystals of Tb2Al3Si2
Using x-ray diffraction and Rietveld Refinement to determine the monoclinic structure of Tb2Al3Si2
We studied complex magnetic properties showing the temperature and external field dependence of them
We show large anisotropic MR in Tb2Al3Si2
Notes: Successfully grown nice large single crystal
Studied structural properties
Complex magnetic properties
Large Anisotropic MR in Tb2Al3Si2