## Slide 1: High Entropy Alloys: Transition Metal Doping of Ba(Fe)2As2
Yash Anand1, Prathum Saraf1, Dan Sokratov1,Ram Kumar1 Johnpierre Paglione1
1Quantum Materials Center, Physics Department, University Of Maryland

## Slide 2: Overview
Background
Methodology
Data Analysis
Conclusion
Reference

## Slide 3: Overview
Background
  High Entropy Alloys
  Non-Fermi Liquid Behavior
  Motivation
Methodology
Data Analysis
Conclusion
Reference

## Slide 4: High Entropy Alloys (HEA)
Definition:
HEA are defined as materials with 4-5 equiatomic elements
This allows disorder to not be a weak perturbation but the leading energy scale in synthesis
High Entropy Effect:
  In Gibbs Free Energy equation, entropy wins leading to the phases becoming highly competitive for equilibrium state and more stable especially at high temperatures
Severe Lattice Distortion Effect:
  Due to the mix of multi-principal elements lattice gets deformed, leading to some of the interesting physical properties
4 Core effects:
Sluggish Diffusion Effect:
  Due to the multiple principal elements, the lattice potential energy varies from one point to another, leading to different atomic diffusions
Cocktail Effect:
  The microstructures and properties are determined by not only the composite materials, but also the different separate lattices

## Slide 5: Fermi Liquid Behavior
Perturbatively adding interaction to the non-interacting fermi gas model
Electrons behave like quasiparticles
At low temperatures the resistivity follows a quadratic rule
Most metals at low temperatures
https://doi.org/10.1016/j.jallcom.2006.09.157

## Slide 6: Non-Fermi Liquid Behavior
Metals where the interactions between electrons can't be treated as a small perturbation
One place where we see NFL is near quantum critical points (smooth phase transition at absolute zero due to quantum fluctuations)
One key identifier of NFL is linear temperature dependence of resistance
https://en.wikipedia.org/wiki/File:QuantumPhaseTransition.svg

## Slide 7: Ba(TM)2As2 Parent Compound

## Slide 8: Past Results

## Slide 9: Overview
Background
Methodology
  Synthesis
  Spectroscopy
Data Analysis
Conclusion
Reference

## Slide 10: Synthesis: Transition Metal Arsenides
Stoichiometric ratio of 1.01:1 TM:As in Aluminum crucible
Two different growth profiles:
  Cr and Mn flux profile is seen in figure (a)
  Fe and Co flux profile is seen in figure (b)
Fig (a)
Fig (b)

## Slide 11: Synthesis: Quadra- and Penta-Doped Sample
We used an equiatomic ratio of the As-Flux with Ba
Used the following profile for the sample growth

## Slide 12: Synthesis: Quadra-Doped Sample Ba(CrFeCoNi)2As2

## Slide 13: Synthesis: Penta-Doped Sample Ba(CrMnFeCoNi)2As2

## Slide 14: Spectroscopy: X-Ray Diffraction (XRD)
XRD:
  Powder the crystals into fine grains
  Uses monochromatic X-rays
  Using X-ray diffraction peaks we can determine if the sample is the desired material
  Very useful for characterizing and confirming As flux
Issues:
  Does not tell you of the elemental composition of sample
  Needs the sample to be previously grown/studied
  Powder XRD destroys the sample

## Slide 15: Spectroscopy: Energy-Dispersive X-ray Spectroscopy (EDS)
EDS:
  Bombards sample with electrons to get characteristic x-rays of the elements in the sample
  Uses full single crystal, so sample isn’t destroyed
  Gives the elemental composition of the sample
Issues:
  Doesn’t tell us about the crystal structure
https://nano.oxinst.com/campaigns/what-is-eds/edx

## Slide 16: Spectroscopy: X-Ray Fluorescence (XRF)
XRF:
  Bombards sample with x-rays to excite inner level electrons, creating vacancies that get filled by outer shell electrons releasing characteristic x-rays
  Uses polychromatic x-rays
  Uses single crystal
  Gives the elemental composition of the sample
Issues:
  Doesn’t tell us the crystal structure
Difference between XRF and EDS:
  XRFs can go deeper into the sample while EDS looks at the surface of the sample

## Slide 17: Overview
Background
Methodology
Data Analysis
  Spectroscopy
  Transport
  Magnetization
Conclusion
Reference

## Slide 18: XRD: Transition Metal Arsenide
FeAs flux
CrAs flux

## Slide 19: XRD: Transition Metal Arsenide
MnAs flux
CoAs flux

## Slide 20: XRD: Penta-Doped Air Sensitivity

## Slide 21: XRD: Quadra and Penta Doping

## Slide 22: EDS: Quadra Doping
Element | Weight % | Atomic %
As | 38.97 | 40.60
Ba | 30.14 | 17.13
Cr | 3.05 | 4.58
Fe | 10.38 | 14.51
Co | 8.09 | 10.72
Ni | 9.36 | 12.45

## Slide 23: XRF: Penta Doping
Element | Weight % | Atomic %
As | 22.606 | 25.059
Ba | 45.305 | 27.399
Cr | 5.488 | 8.766
Mn | 5.424 | 8.200
Fe | 8.952 | 13.313
Co | 6.011 | 8.471
Ni | 6.214 | 8.793

## Slide 24: Transport: Quadra Doped
Linear in temperature resistivity
We see deviation at around 5K
Linear fit: R = 3.3(7)*10-9*T+3.0(5)*10-6

## Slide 25: Transport: Penta Doped
Resistance has an inverse relation to temperature
We see linear behavior between 200 and 300 K

## Slide 26: Magnetization: Penta Doped
We see about two transitions:
  40 K in both ZFC and FCC
  30 K which leads to bifurcation
We see bifurcation even at 7T
At 7T all the transitions seem to merge at 5K

## Slide 27: Magnetization: Penta Doped
Seems ferrimagnetic rather than ferromagnetic since there is no saturation
At 20K, the hysteresis goes away, indicating an antiferromagnetic transition

## Slide 28: Overview
Background
Methodology
Data Analysis
Conclusion
Reference

## Slide 29: Conclusion
We have seen non-Fermi liquid behavior in the quadra doped sample
Adding 5 elements makes the material insulating
There are interesting magnetic properties that arise from the penta doping
  Hinting at spin glass due to the bifurcation in ZFC and FCC
  Hysteretic behavior hinting towards Ferrimagnetic ordering

## Slide 30: Overview
Background
Methodology
Data Analysis
Conclusion
Reference

## Slide 31: References
A. J. Schofield (1999) Non-Fermi liquids, Contemporary Physics, 40:2, 95-115, DOI: 10.1080/001075199181602
Nakajima, Y., Metz, T., Eckberg, C. et al. Quantum-critical scale invariance in a transition metal alloy. Commun Phys 3, 181 (2020). https://doi.org/10.1038/s42005-020-00448-5
Sales, B.C., Jin, K., Bei, H. et al. Quantum critical behavior in the asymptotic limit of high disorder in the medium entropy alloy NiCoCr0.8 . npj Quant Mater 2, 33 (2017). https://doi.org/10.1038/s41535-017-0042-7
Solveig S. Aamlid, Mohamed Oudah, Jörg Rottler, and Alannah M. Hallas Journal of the American Chemical Society 2023 145 (11), 5991-6006 DOI: 10.1021/jacs.2c11608